CLEMENTE ASSOCIATES INC., 33 HARKNESS DRIVE, MADISON, CT 06443 PHONE 203 421 4500 E MAIL   clemasso@gmail.com

www.clemente-associates.com

Catalog #:	Mag-AG-0.05 µ    0.050 micron magnetic beads with Silver attached

Core of particles:	Magnetite Fe3 O4

Mg/ml			0.25

Particle Shape/Size:	 spherical shaped particles composed of 10 nm crystals.

SURFACE AREA:		> 24 m2/gram

# of particles:		 >1015 particles/gram

:

SUSPENSION:	  Distilled water

Specificity:

|  | Effect of Magnetic Silver Beads on E. coli |
| --- | --- |
|  | Time-Minutes | 1mcg/ml | 10 mcg/ml |
|  | 0 | 6.6x1010 | 0 |
|  | 30 | 1.87x104 | 0 |
|  | 60 | 2.0x104 | 0 |
|  | 120 | 1.99x103 | 0 |
|  | 240 | 0 | 0 |
|  | Data are CFU per ml |  |

.

Shelf Life:	 8 months

Covers from 7-10 Meters of food processing line